## Slide 1
Bayesian Linear Regression of Simulated Diffraction Measurements for Residual Stress Analysis
Student: Farah Hassan
Academic Supervisor: Dr. Matthew Peel
Notes: To do:
Audio

## Slide 2
Project Aims: Can Bayesian Regression Aid in the Stress Analysis of Nuclear Materials?
Context: Stress Analysis using Diffraction
Procedure: Simulating then Fitting Strain ‘Measurements’ using Bayesian Linear Regression
Results: Comparing Bayesian to the Industry Standard, Least Squares
Implications of Bayesian Regression for the Nuclear Industry
Agenda
Notes: To do:
Audio
Review order

## Slide 3
Project Aims
The project aims to determine whether Bayesian linear regression of X-Ray diffraction measurements can aid in the stress analysis of materials with complex grain structures.
Notes: To do:
Audio
What is Baysian (Quick)

## Slide 4
Bragg Diffraction1
Context: Stress Analysis Using Diffraction
Notes: To do:
Audio
Animations?

## Slide 5
Bragg Diffraction1
Context: Stress Analysis Using Diffraction
Goniometer2
Notes: To do:
Audio
Animations?

## Slide 6
Bragg Diffraction1
Context: Stress Analysis Using Diffraction
Goniometer2
Sample Co-ordinates3
1. H. P. Myers (2002). Introductory Solid State Physics. Taylor & Francis.
2. He, B. B., 2009. Two-Dimentional X-Ray Diffraction. 1 ed, page: 140
3. He, B. B., 2009. Two-Dimentional X-Ray Diffraction. 1 ed, page: 262
Notes: To do:
Audio
Animations?

## Slide 7
εφψ
Context: Stress Analysis Using Diffraction
Strain for one location, εφψ
If 6 locations are measured, this equation can be solved using linear regression to obtain a stress tensor.
He, B. B., 2009. Two-Dimentional X-Ray Diffraction. 1 ed, page: 262
Notes: To do:
Audio
Referencing

## Slide 8
εφψ
Context: Stress Analysis Using Diffraction
Stress Coefficients, Pij
These oscillate with the detector angle, γ, and incorporate the material’s macroscopic constants.
Strain for one location, εφψ
If 6 locations are measured, this equation can be solved using linear regression to obtain a stress tensor.
He, B. B., 2009. Two-Dimentional X-Ray Diffraction. 1 ed, page: 262
Notes: To do:
Audio
Referencing

## Slide 9
εφψ
Context: Stress Analysis Using Diffraction
Stress Coefficients, Pij
These oscillate with the detector angle, γ, and incorporate the material’s macroscopic constants.
Stress Tensor Components, σij
Strain for one location, εφψ
If 6 locations are measured, this equation can be solved using linear regression to obtain a stress tensor.
He, B. B., 2009. Two-Dimentional X-Ray Diffraction. 1 ed, page: 262
Notes: To do:
Audio

## Slide 10
Context: Origin of Uncertainties in Measurements
Withers, P.J. and Bhadeshia, H.K.D.H. (2001). Residual stress. Part 1 – Measurement techniques. Materials Science and Technology, 17(4), pp.355–365.
Nuclear materials have non-uniform grain structures.
There is variation in intergranular stress.
If a large grain has an abnormally high or low stress, the intensity of the skewed peak will be high, overshadowing smaller, more representative grains.
Bramble, S., Flemming, R. and Mccausland, P. (2014). GRAIN SIZE, “SPOTTY” XRD RINGS, AND CHEMIN: TWO-DIMENSIONAL X-RAY DIFFRACTION AS A PROXY FOR GRAIN SIZE MEASUREMENT IN PLANETARY MATERIALS. M.
Notes: To do;
Audio

## Slide 11
Project Aims
Criteria for Success:*
Accuracy of Stress estimate
Representation of Confidence Intervals
Ease of Implementation
* Relative to Least-Squares regression
The project aims to determine whether Bayesian linear regression of X-Ray diffraction measurements can aid in the stress analysis of materials with complex grain structures.
Notes: Key Points:
Reasons why Bayesian may be more useful than the industry standard, which is OLS
Can be made to be less sensitive to outliers
NOT NECESSARILY NORMALLY DISTRIBUTED ERRORS
Returns a full distribution, rather than a single value with standard deviation
THE RESULT IS NOT NECESSARILY NORMALLY DISTRIBUTED
Better understanding of errors.
Criteria:
results needs to be as good as OLS, minimum
Confidence intervals and errors need to be more representative of true uncertainty
Practicality is important for the industry.
To do:
Audio.

## Slide 12
Methodology
A strain distribution was generated using a known stress tensor.
Noise was added to the strain, creating “strain measurements”.
The result was analysed in reference to the original stress tensor.
Using linear regression, stress tensor components were solved for.
True strain distribution.
σ11 = 150, σ12 = 30, σ22 = 50 MPa
Notes: To do:
Audio

## Slide 13
Methodology
1. A strain distribution was generated using a known stress tensor.
2. Noise was added to the strain, creating “strain measurements”.
3. The result and uncertainty was analysed in reference to the original stress tensor.
4. Using linear regression, stress tensor components were solved for.
True strain distribution.
σ11 = 150, σ12 = 30, σ22 = 50 MPa
Notes: To do:
Audio

## Slide 14
A strain distribution was generated using a known stress tensor.
Noise was added to the strain, creating “strain measurements”.
The result was analysed in reference to the original stress tensor.
Using linear regression, stress tensor components were solved for.
Methodology
Notes: KEY POINTS:
Recall that strain oscillates with detector angle.

## Slide 15
A strain distribution was generated using a known stress tensor.
Noise was added to the strain, creating “strain measurements”.
The result was analysed in reference to the original stress tensor.
Using linear regression, stress tensor components were solved for.
Methodology
Least-Squares fitted strain distribution. σ11 = 150.6, σ12 = 30.23, σ22 = 47.2 MPa
Notes: To do:
Audio
Fix label
Add s11

## Slide 16
Least-Squares Regression
Methodology
Bayesian Regression
Prior Distribution
Likelihood Function
Notes: To do:
Audio
Mention stacks

## Slide 17
Effect of Prior Distribution
Prior stress = 0 MPa
Prior stress = 150 MPa (= true stress)
Prior stress = 300 MPa
Notes: To do:
Audio
Measurements with more variation lead to fits which are more influenced by the prior distribution
For this case plateu at around 100- 200 , so we know that if a numerical prior is set in that region it will not skew the results.

## Slide 18
Bayesian VS Least-Squares:
Normally Distributed Likelihood
Stress Tensor Component | True Stress, MPa | Bayesian Fitted Stress, MPa | Error, Std dev. | Least-Squares Fitted Stress, MPa | Error, Std dev.
s11 | 150 | 144.7 | 101.7 | 145.5 | 91.12
S22 | 50 | 1.4 | 102.1 | -0.6 | 91.12
s12 | 30 | 143.1 | 60.4 | 142.8 | 56.7
Notes: To do:
Audio
95% confidence interval
Emphasise that if it was another distribution with the same noise the result would be off by a different amount and potentially in a different direction.

## Slide 19
Bayesian VS Least Squares:
Normally Distributed Likelihood
Stress Tensor Component | True Stress, MPa | Bayesian Fitted Stress, MPa | Error, Std dev. | Least-Squares Fitted Stress, MPa | Error, Std dev.
s11 | 150 | 204.1 | 28.8 | 204.3 | 34.9
S22 | 50 | 94.5 | 29.5 | 93.6 | 34.9
s12 | 30 | 27.4 | 20.0 | 27.3 | 21.7
Notes: To do:
Audio
95% confidence interval
Emphasise that if it was another distribution with the same noise the result would be off by a different amount and potentially in a different direction.

## Slide 20
Bayesian VS Least-Squares:
Student_t Likelihood Function
Least-Squares’ fitted stress is not only less accurate than Bayesian’s, but more certain that it is correct.
The ability to see this bi-modal distribution is valuable. There is a possibility that the outliers are correct.

## Slide 21
Conclusions
If the prior is non-restrictive, numerical changes in the prior distribution have a marginal effect on Bayesian fit outcomes, relative to changes in likelihood function.
With a Normally distributed likelihood function and a non-restrictive prior, Bayesian regression yields similar results to Least-Squares.
Robust Bayesian regression, wherein the likelihood function is a student_t distribution, can yield more accurate results as it has more success in handling outliers.
Bayesian can be used to better understand uncertainties, which can lead to variation in operational life estimates for nuclear materials.
Notes: Numerical changes in the prior distribution have a marginal effect on the fit outcomes relative to changes in the type of distribution of the likelihood function.
Bayesian fitting without a restrictive prior or a likihood function which isn’t normal is just like OLS
Robust Bayesian fitting, wherein the likelihood function is not Normally Distributed can yield more accurate results than OLS with more realistic confidence intervals
This has been the case in measurements with extreme outliers3.
3. In the nuclear Industry, Bayesian can be used to better understand confidence intervals, which can lead to significant variations in operation life of materials.
To do:
Slide
Audio

## Slide 22
Thank you